## Slide 1: Crystal and X-ray Diffraction
Wei-Li Chen
2014/01/20
Department of Electronic Engineering
National Changhua University of Education
Part I

## Slide 2: Crystal Structure
Crystal = Lattice + Basis
Lattice: an infinite periodic array of geometric points in space. 14 distinct lattices.
Basis: identical group of atoms
Unit cell: the most convenient small cell in a crystal structure that carries the characteristics of the crystal. The repetition of the unit cell in three dimensions generates the whole crystal structure.
Primitive unit cell: the smallest unit cell (not necessarily unique)

## Slide 4
7 Crystal Systems (unit cell geometry) and 14 Bravais Lattices
A point represent a basis

## Slide 5: Face Center Cubic

## Slide 6: Body Center Cubic (BCC)

## Slide 7: Hexagonal Close-Packed

## Slide 8: Diamond and Zinc Blende Unit Cell (FCC)

## Slide 9: Rock Salt Crystal (FCC)

## Slide 10: Lattice Parameters, Directions, and Planes in Crystal
Lattice parameters α,β,γ, a, b, and c represent the geometry of the unit cell
[u v w] direction in crystals
<u v w> family of directions
(h k l) Miller indices of a plane
{h k l} family of planes

## Slide 12
Intercept x0, y0, z0 are 1/2a, 1b, ∞c
Intercept x, y, z in terms of a, b, c are ½, 1, ∞
Reciprocals 1/1/2, 1/1, 1/ ∞ = 2, 1, 0
The Miller indices are (2 1 0)
If the interception is in the negative direction, the Miller indices are
. .
(2 1 0)
For cubic crystal, interplanar distance
For tetragonal (hexagonal) crystal, interplanar distance

## Slide 13: Planes of a Zone
Planes of a zone are planes which are all parallel to one line. The line is called zone axis, and the set of planes are called the zone.

## Slide 14: X-ray Tube

## Slide 15: X-ray Emission Spectrum by Electron Bombardment
Continuous
emission
Characteristic
emission

## Slide 16: Continuous Emission
Continuous spectrum emitted by decelerated electrons is called heterochromatic radiation or white radiation (bremsstrahlung radiation)
Short wavelength limit

## Slide 17: Characteristic Emission
High intensity
Narrow line width
Fixed wavelength
Fall into several groups referred as
K, L, M, N…

## Slide 18: Bragg Diffraction
Consider rays 1’ and 1a’ from the same plane
QK – PR = PKcosθ – PKcosθ = 0
Consider rays 1’ and 2’ from adjacent planes
ML + LN = d’sinθ + d’sinθ
Constructive interference
2d’sinθ=nλ
is called Bragg condition

## Slide 19: Diffraction Methods
 | λ | θ
Laue method | Variable | Fixed
Rotating-crystal method | Fixed | Variable
Powder method | Fixed | Variable

## Slide 20: Laue Method
Diffraction spots from zone planes of same zone axis (ZA) located on a curve of ellipse or hyperbola
Detection film can be behind it (transmission) or in front of the crystal (back reflected)

## Slide 21: Laue Method

## Slide 22: Laue Diffraction Spots (λFixed)

## Slide 23: Powder Method
Fine powders of fine crystals oriented in various directions
The powder is equivalent to a single crystal rotated about all possible axes

## Slide 24: Debye-Scherrer Powder Method

## Slide 25: Rotating-Crystal Method
A single crystal is rotating about an axis normal to the incident monochromatic X-ray beam
Planes satisfying Bragg condition form spots on the film mounted on the cylinder wall

## Slide 26
X-ray tube
Göbel mirror
Channel-cut monochromator
Sample
Motorized slit
Detector
Channel-cut analyzer
Automatic absorber
X-ray Rocking Curve Setup

## Slide 27: High resolution X-ray diffractometer
Omega (ω), chi (χ), phi (φ) and 2 theata (2θ) rotation axis :
x
y
z
Χ rotation in y-z plane
Ωand 2θ
Φ scan around y-axis

## Slide 28
X-ray tube
Gobel mirror
monochromators
sample
detector
sample
detector
D5000 Discover
To filter out Kα2 and keep Kα1

## Slide 29
y